## Slide 1
Moisture’s Significant Impact on Twisted Polymer Actuation
Diego R. Higueras-Ruiz, Ph.D. Student
Dr. Heidi P. Feigenbaum, Associate Professor
Dr. Michael W. Shafer, Assistant Professor

## Slide 2
Outline:
Introduction to Twisted Polymer Actuators
Mechanics of Actuation
  Microstructure of the precursor monofilament
  Principle of thermal actuation
  Principle of hygroscopic actuation
Moisture Absorption and Desiccation Behavior
Moisture Effects on Thermal Actuation
  Axial Thermal Contraction and Elastic Modulus
  Moisture Content Effects on STPAs and TCPAs
Hygroscopic Actuation
Conclusions

## Slide 3
Introduction to Twisted Polymer Actuators
Charles Q. Choi
Straight twisted polymer actuator (STPA)
Twisted coiled polymer actuator (TCPA)
1.14 mm
0.99 mm
Inexpensive active material
Thermally driven
Develop forces a hundred times stronger that can human muscle of same length and weight [Haines et al.]
They can contract about 50% [Haines et al.]
High specific work (2.48 kJ/kg), [ Haines et al.]
Linear and torsional actuation

## Slide 4
Amorphous
  Microstructure. Thermal Actuation
Crystallite
Interfibrillar
tie chains
Microfibrillar
Untwisted Monofilament
Straight-twisted polymer actuator (STPA)
Heated drawn polymer monofilament expands radially and contract axially
Thermal Actuation
ΔT
High stiffness internal fibers helically orientated cause shear deformation
Twisted-coiled Polymer Actuator (TCPA)
ΔT
ΔT
The thermal torsional response of STPA translates to contraction of TCPA.
Contraction
Torsion

## Slide 5
Voids
Unbonded
H₂O molecules
(free volume)
Bonded
H₂O molecules
(polymeric matrix)
Untwisted Monofilament
Straight-twisted polymer actuator (STPA)
Twisted-coiled Polymer Actuator (TCPA)
Contraction
Torsion
ΔM (%)
ΔM (%)
ΔM (%)
Bounded H₂O molecules cause high radial and low axial expansion by swelling
Bounded H₂O molecules cause untwist due to the new twisted fiber orientation
Hygroscopic Actuation
Torsional response of STPA translates to contraction of TCPA due to the swelling in the material
  Microstructure. Hygroscopic Actuation

## Slide 6
Moisture Absorption and Desiccation Behavior

## Slide 7
Fast
Absorption
Response
Moisture Absorption and Desiccation Behavior

## Slide 8
  Axial Thermal Contraction and Elastic Modulus
Sample
Rheometer
Bi-directional Motion
Monofilament Clamps
Laser Vibrometer
Manual
Temperature
Control
Displacement signal
Thermal Camera
Temperature signal
Heat Gun
Sample

## Slide 10
  Moisture Content Effects on STPAs and TCPAs
Torque Spool (6mm dia.)
STPA
Collet
Laser Vibrometer
Frame
Bearing
Weight 1
Heat Gun
Thermal Camera
Laser Vibrometer
Manual
Temperature
Control
Displacement signal
Thermal Camera
Temperature signal
Heat Gun
TCPA
Load

## Slide 11
  Moisture Content Effects on STPAs and TCPAs

## Slide 12
  Moisture Content Effects on STPAs and TCPAs

## Slide 13
Hygroscopic Actuation
H₂0
STPA
Humid Environment
Hygroscopic Actuation
Camera
Actuation
Indicator Flag
Transparent Environmental Chamber
Collet
Water Reservoir

## Slide 14
Hygroscopic Actuation